Pengaruh Kecepatan Agitasi terhadap Tingkat DemineralIsasi Kulit Udang Pada Tahapan Ekstraksi Kitin Secara Biologis

Junianto

Fakultas Perikanan dan Ilmu Kelautan Universitas Padjadjaran,

Jl Raya Jatinangor KM 21, Ujung Berung – Bandung 40200

E-mail: anto_lisc@yahoo.com

ABSTRAK

Proses demineralisasi adalah salah satu tahapan ekstraksi kitin dari kulit udang. Pada penelitian ini, proses demineralisasi dilakukan secara biologis melalui fermentasi asam laktat. Isolat bakteri yang digunakan adalah  Lactobacillus acidophillus FNCC 116. Penelitian ini bertujuan untuk menentukan kecepatan agitasi untuk memperoleh tingkat penghilang mineral yang maksimal pada proses demineralisasi kulit udang.  Percobaan dilakukan dengan rancangan acak lengkap yang terdiri dari tiga perlakuan kecepatan agitasi yaitu 0, 50, dan 100 putaran per menit (rpm). Setiap perlakuan diulang sebanyak empat kali.  Hasil penelitian menunjukkan bahwa kecepatan agitasi untuk mendapatkan tingkat penghilang mineral maksimal pada proses demineralasasi kulit udang adalah 50 rpm. Tingkat penghilangan mineral dinyatakan dengan tingkat penurunan kandungan abu; dimana pada kecepatan agitasi 50 rpm, penurunan kandungan abunya 97,42%.

Kata kunci :  Demineralisasi, kitin, kulit, udang, biologis.

THE EFFECT OF AGITATION VELOCITY ON THE SHRIMP SHELLS DEMINERALIZATION LEVEL AT BIOLOGICALLY STEP OF CHITIN EXTRACTION

ABSTRACT

Demineralization process is one step of chitin extraction from shrimp shells and its was done with lactic acid fermentation.  Lactobacillus acidophillus FNCC 116 was used for this fermentation process. The objective of research is to determine the velocity of agitation for finding the level of removed mineral from the shrimp shells. Completely randomized block designwas used with three  level of agitation treatments, that was 0,50, and 100 rpm. The result of the research showed that the 50 rpm of agitation could remove the  mineral content of shrimp shells maximally.The level of removed mineral was declared as the ash content. Where at the 50 rpm agitation, the ash content reduction was 97.42%.

Key words :  Demineralization, chitin, shells, shrimps, biologically.